SECTION 04 23 13

THIN BRICK

- GENERAL SECTION INCLUDES

- Thin brick veneer

- RELATED SECTIONS

- Section 03-4500 Precast Architectural Concrete.

- Section 03-4713 Tilt-Up Concrete.

- Section 04-2616 Thin Brick.

- REFERENCES

- ASTM C 67 - Standard Test Methods for Sampling and Testing Brick and

Structural

Clay Tile.

- ASTM C 1088 - Standard Specification for Thin Veneer Brick Units Made from Clay

or Shale.

C.             For embedded applications, see Precast Concrete Institute (PCI) and Tilt-Up

Concrete Association (TCA)

- SUBMITTALS

- Submit under provisions of Section 01 30 00 - Administrative Requirements.

- [Product Data]: Manufacturer's catalog data, detail sheets, and printed installation

instructions.

- Selection Samples: For each product requiring color/texture selection, provide full

size samples for final selection.

- Verification Samples: For each product, color, and texture selected, provide two

full-size units representing actual color and texture of products to be installed.

- SAMPLE PANELS

- Construct sample panel at location indicated or directed, and as follows:

- Size: 4 feet by 4 feet (1.2 m by 1.2 m).

- Include all unit types and sizes to bused, and mortar joint treatment.

- Obtain architect's acceptance of sample panel before beginning construction

activities of this section.

- Do not remove sample panel until construction activities of this section have been

accepted by architect.

- DELIVERY, STORAGE, AND HANDLING

- Deliver products of this section on pallets, with individual faces protected; keep

dry.

- Store units in protected area or under cover on level ground; keep dry. Do not

double-stack pallets.

- PRODUCTS

- MANUFACTURERS

- Acceptable Manufacturer: Endicott  Thin Brick, LLC., which is located at:

57120 707th Rd.; Endicott, NE 68350

Tel: 402-729-3315

Website: http://www.endicott.com

- Requests for substitutions will be considered in accordance with provisions of

Section 01 60 00 - Product Requirements.

- Substitutions: Not permitted.

- MATERIALS

- Thin Brick: ASTM C 1088, Type TBX or TBS, tested in accordance with ASTM

C67, as manufactured by Endicott Thin Brick, LLC. And PCI/TCA specifications.

1. Size: 2-1/4” (57.2 mm) high, 7-5/8” (193.7 mm) long, ½” (12.7 mm) thick

2. Size: 2-1/4” (57.2 mm) high, 11-5/8” (295.3 mm) long, ½” (12.7mm) thick

3. Size: 2-1/4” (57.2mm) high, 15-5/8” (396.875 mm) long, 1” (25.4 mm) thick*

4. Size: 3-5/8” (92.1 mm) high, 7-5/8” (193.7 mm) long, ½” (12.7 mm) thick

5. Size: 3-5/8” (92.1 mm), 11-5/8” (295.3 mm) long, ½” (12.7 mm) thick

6. Size: 3-5/8” (92.1 mm), 15-5/8” (396.875 mm) long, 1” (25.4 mm) thick*

7. Size: 7-5/8” (193.7 mm) high, 7-5/8” (193.7 mm) long, ½” (12.7 mm) thick*

8. Size: 1-5/8” (41.3 mm) high,11-5/8” (295.3 mm) long, ½” (12.7mm)thick

9. Size: 2-5/8” (66.675 mm) high, 9-5/8” (244.475 mm) long, ½” (12.7) thick

*(sizes only available in certain colors, please confirm with Endicott)

a. Texture: Smooth (1/2”’ 5/8” and 1” thickness)

b. Texture: Velour (1/2” and 1” thickness only)

c. Texture: Artisan ** (please confirm size with Endicott)

d. Texture: Matt ** (please confirm size with Endicott)

e. Texture: Vertical score ** (please confirm with Endicott)

f. Texture: Sand Finish ** (please confirm with Endicott)

g. Texture: Glazed (1/2” only)

Approved Color: ___________________________

- Trim Units: Matching thin brick.

- Edge cap A – 3-5/8” bed (92.1 mm),   7-5/8” (193.7 mm) long,   2-1/4” face

- Edge cap B – 3-5/8” bed (92.1 mm),   11-5/8” (295.3 mm) long, 2-1/4” face

- Edge cap C – 3-5/8” bed (92.1 mm),   7-5/8” (193.7 mm) long,   3-5/8” face

- Edge cap D – 3-5/8” bed (92.1 mm),   11-5/8” (295.3 mm) long, 3-5/8” face

- Edge cap E – 2-1/4” bed (57.2 mm),   7-5/8” (193.7 mm) long,    2-1/4”face

- Edge cap F – 2-1/4” bed (57.2 mm),   11-5/8” (295.3 mm) long,  2-1/4” face

- Edge cap G – 3-5/8” bed (92.1 mm),  11-5/8” (295.3 mm) long,  1-5/8” face

- Edge cap H – 1-5/8” bed (41.3 mm),  11-5/8” (295.3 mm) long,  1-5/8” face

C.             Corners: Matching thin brick

1. BC1-5/848: 1-5/8” (41.275mm) face, 11-5/8” (295.3mm) long, ½” (12.7mm) thick

2. BC2-1/448: 2-1/4” (57.2mm) face, 7-5/8” (193.7mm) long, ½” (12.7mm) thick

3. BC2-5/8310:  2-5/8” (66.675mm) face, 9-5/8” (244.475mm) long, ½” (12.7mm) thick

4. BC448:  3-5/8” (92.1mm) face, 7-5/8” (193.7mm) long, ½” (12.7mm) thick

5. BC848:  7-5/8” (193.7mm) face, 7-5/8” (193.7mm) long, ½” (12.7mm) thick

6. BC1-5/8412:  1-5/8” (41.275mm) face, 11-5/8” (295.3mm) long, 1” (25.4mm) thick

7. BC2-1/4412:  2-1/4” (57.2mm) face, 11-5/8” (295.3mm) long, 1” (25.4mm) thick

8. BC4412:  3-5/8” (92.1mm) face, 11-5/8” (295.3mm) long, 1” (25.4mm) thick

- EXECUTION

- INSTALLATION

- Install thin brick in accordance with BIA Technote 28C or appropriate industry

standards.

Reference system manufacturer's printed instructions, approved submittals and in

proper relationship with adjacent construction.

END OF SECTION